Investigation of AlGaN/GaN HEMTs with step aluminum mole fraction and doping level in the barrier layer

S. M. Razavi

Faculty of engineering

University of Birjand

Email: m.136287@gmail.com

S.H. Zahiri

Department

University of Birjand

Email: email address

S.E. Hosseini

Department

Ferdowsi University of Mashhad

Email: email address

Abstract - Gallium-nitride (GaN) high electron mobility transistors (HEMTs) with step aluminum mole fraction or doping concentration in the barrier is reported. The barrier layer is divided into two Source Side (SS) and Drain Side (DS) parts with the same lengths and thicknesses, but with different aluminum mole fraction or doping levels. Average of the aluminum mole fraction or doping concentration in the barrier is equal to those in the conventional structure. Changes that happen in the maximum lateral electric field, breakdown voltage, maximum DC trans-conductance (gm), drain current, gate-source capacitance, cut off frequency and DC output conductance (go) as a function of different source side (NSS) and drain side (NDS) barrier doping levels or different aluminum mole fractions at source side (XSS) and drain side (XDS) are studied in details. Simulation results illustrate that a smaller NDS compared to NSS improves the breakdown voltage. On the other hand, decreasing NSS, reduces the gate-source capacitance and DC output conductance. With varying NSS and NDS, the DC trans-conductance has a nonlinear variation. Also, proposed structures with smaller XSS than XDS reduces the maximum lateral electric field and then improve the breakdown voltage and go.

Index Terms- GaN HEMT, Gate-source capacitance, Breakdown voltage, DC output conductance, maximum DC trans-conductance.

# Introduction

Gallium nitride high-electron mobility transistors (HEMTs) are great candidates in the field of high-power electronics [1-6]. AlGaN/GaN HEMTs have received much attention for high-power and high frequencies applications because of a high breakdown field in the wide-band gap semiconductors are capable of the high temperature applications [7-8]. In addition to that, a large conduction band discontinuity between GaN and AlGaN and the presence of polarization fields allow a large two-dimensional electron gas (2-DEG) concentration to be confined [9-10]. Improving DC and RF characteristics of these devices is a very important challenge for researchers in this field. In this work, a novel AlGaN/GaN HEMT with step aluminum mole fraction or doping concentration in the barrier is reported. The most important DC and RF parameters of AlGaN/GaN HEMT with different aluminum mole fraction or doping level in the barrier at source and drain sides are explored and compared with those in the conventional [11]. Gate-source capacitance, maximum lateral electric field, breakdown voltage, DC output conductance (go), maximum DC trans-conductance (gm), cut off frequency (fT) and drain current of the proposed structures are simulated using atlas simulation software. In the next section, the proposed structure dimensions and the physical models used in the 2-D simulation are described in details. In the third section, we first explain how the barrier layer with step aluminum mole fraction or doping concentration in the HEMT will reduce the maximum lateral electric field in the channel and consequently improve breakdown voltage significantly. Also, in this section, the effect of step mole fraction or doping level in the barrier on the drain current, gate-source capacitance, maximum DC trans-conductance, cut off frequency and output conductance of the proposed structure are studied and compared with those in the conventional in details.

# Device Structures

Schematic cross-sections of the proposed and conventional [11] structures are shown in Figures 1(a) and (b), respectively. The dimensions of the structures are as follows: gate length Lg=0.5µm, gate-drain spacing Lgd=1µm, gate-source spacing Lgs=1µm. Barrier layer and channel thicknesses are TB=22nm and TC=1.5µm, respectively. The barrier layer in the conventional structure is n-type heavily doped Al0.32Ga0.68N while in the proposed structures, doping and aluminum mole fraction in this layer are varied in the source and drain sides. The channel layer of conventional and proposed structures is an intrinsic GaN. Nickel is chosen for the gate Schottky contact with a work function of 5.1eV. It is worth noting that the proposed and conventional structures can be fabricated using the same procedure as reported in [11]. The devices are simulated using two dimensional ATLAS software[12]. In order to achieve more realistic results, several models are activated in simulations, including the ‘SRH’ model for Shockley–Read–Hall recombination, the ‘Conmob’ model for standard concentration dependent mobility, the ‘Fldmob’ model for parallel electric field-dependent mobility and the ‘Fermi Dirac’ model for statistics[13-14].

Fig. 1(a)

Fig. 1(b)

Fig. 1. Cross section of the (a) proposed and (b) conventional structures.

# Results And Discussions

## Electric Field

Lateral electric field in the channel at VDS=80V and VGS=-4V for different NSS and NDS at a fixed value of XSS and XDS (0.32) is shown in figure 2(a). The electric field curve with NSS=NDS=1×1018cm-3 corresponds to the conventional structure. To get a meaningful comparison between the proposed and conventional structures, average of NSS and NDS in the proposed structures is equal to that in the conventional (1×1018cm-3). It is clear from this figure that decreasing NDS in the proposed structures reduces the maximum lateral electric field at the gate corner near the drain compared to the conventional structure. A further investigation shows that the breakdown happened at gate corner near the drain due to the electric field crowding [15-16]. Hence, it can be deduced that the structure with smaller NDS compared to NSS has a larger breakdown voltage than that in the conventional structure. Critical electric field of the GaN (3.5MV/cm) is used to clarify the breakdown voltage [17]. Increasing the drain-source voltage increases the maximum electric field in the channel. The breakdown voltage is nominated the drain-source voltage that the maximum electric field in the channel is equal to the critical electric field. It is obvious from the figure 2(a) that the peak electric field in the channel of the structure with NSS=1.5×1018cm-3 and NDS=0.5×1018cm-3 is the least peak electric field in the all structures. So, it can be concluded that this structure can be applied at higher drain-source voltage to get to the critical electric field compared to the other structures. Therefore, this structure has the largest breakdown voltage in the investigated structures. The peak electric field of the proposed structures at VDS=80V is lesser than the critical electric field. Thus, the breakdown voltages of the proposed structures are bigger than 80V. As a result from the simulations, in the structure with NSS=1.5×1018cm-3 and NDS=0.5×1018cm-3, increasing drain-source voltage up to 220V can move up the maximum electric field in the channel to the critical electric field. This voltage (220V) can be listed as the breakdown voltage in this structure. With applying a similar process, the breakdown voltage of the conventional structure is about 90V. As a result, it can be seen that this proposed structure increases the breakdown voltage significantly. The maximum electric field of the structures with bigger NDS compared to the NSS is larger than that in the conventional structure. So, these structures have smaller breakdown voltage than that in the conventional structure. It is worth noting that smaller NDS compared to NSS can be applied to improve the breakdown voltage in the proposed structures. According to the figure 2(b), the structure with XSS=0.22 and XDS=0.42 has the minimum peak electric field in the channel. For this reason, this structure has the maximum breakdown voltage between the structures with different XSS and XDS. However, it is understandable that in these structures, NSS and NDS have the same value (1×1018cm-3). It is obvious from this figure that in the structures with smaller XSS compared to the XDS, the maximum electric field in the channel is lesser than that in the conventional structure. Consequently, it can be deduced that these structures have bigger breakdown voltage than that in the conventional. Also, the peak electric field in the structures with XSS larger than XDS is equal to that in the conventional structure. So, these structures have the same breakdown voltage with the conventional structure.

## Drain Current

Drain currents as a function of drain-source voltages for different NSS and NDS are simulated and compared to those in the conventional structure at VGS=0V in fig. 3(a). As illustrated in this figure, the proposed structures decrease the drain current slightly. Decreased drain currents result from the lower 2-DEG density in the channel due to reduction of the barrier layer density in the source or drain side [11]. However, it is worth noting that the proposed structure with NSS=1.25×1018 cm-3 and NDS=0.75×1018cm-3 has bigger saturated drain current than that in the conventional. In linear region, the drain current of the conventional structure is higher than those in the proposed structures. Hence, the best behavior in the saturated drain current is happened in the discussed proposed structure. Figure 3(b) demonstrates the drain current versus drain-source voltage for different XSS and XDS at VGS=0V in the proposed and conventional structures. The drain current in the proposed structure with XSS=0.37 and XDS=0.27 is equal to that in the conventional structures. So, the maximum drain current is obtained in the proposed structure with XSS=0.37 and XDS=0.27 and conventional. As is evident from this figure, in the proposed structures with lesser XSS than XDS, the drain current is reduced significantly. This is due to small XSS in the source side of the proposed structures that reduces the 2-DEG density in this side and then reduces

Fig. 2(a)

Fig. 2(b)

Fig. 2. Maximum lateral electric field as a function of channel length for (a) different NSS and NDS at a fixed XSS and XDS (0.32) and (b) different XSS and XDS at a fixed NSS and NDS (1×1018cm-3) in the proposed and conventional structures at VGS=-4V and VDS=80V.

the drain current. The minimum drain current is achieved in the structure with XSS=0.22 and XDS=0.42. It is because this structure has the least value of XSS in the proposed structures.

Fig. 3(a)

Fig. 3(b)

Fig. 3. Drain currents with respect to drain voltages for (a) different NSS and NDS at a fixed XSS and XDS (0.32) and (b) different XSS and XDS at a fixed NSS and NDS (1×1018cm-3) in the proposed and conventional structures at VGS=0V.

## Gate-Source Capacitance

Figure 4(a) shows the simulated gate-source capacitances (Cgs) as a function of the frequency for different NSS and NDS at a similar value of XSS and XDS (0.32) at VGS=0V and VDS=20V conditions. The gate-source capacitance in the structure with NSS=NDS=1×1018cm-3 corresponds to the conventional structure. The average of NSS and NDS for different conditions is equal to those in the conventional (1×1018cm-3). According to this figure, a smaller NSS compared to the NDS can be used to decrease the Cgs. Smaller value of NSS decreases net electrons density in the channel at the source side, because the net donor impurities density in the barrier at that side is reduced. This in turn decreases the gate-source capacitance and consequently improves high frequency performance [17]. As is displayed in this figure, the minimum gate-source capacitance is obtained for the structure with NSS=0.5×1018cm-3 and NDS=1.5×1018cm-3. Gate-source capacitances with respect to the frequency for different XSS and XDS at a constant NSS and NDS (1×1018cm-3) are illustrated in the figure 4(b). The average of the XSS and XDS is 0.32. As is evident from this figure, for structures with XSS larger than XDS, the gate-source capacitance has lesser value than that in structures with XSS lesser than XDS. Hence, larger XSS in comparison with XDS can be chosen to reduce the gate-source capacitance. The minimum gate-source capacitance is achieved for the structure with XSS=0.42 and XDS=0.22. As be shown in figures 4(a) and (b), it can be concluded that the structure with smaller NSS compared to NDS and larger XSS compared to XDS can be used to reduce the gate-source capacitance.

## DC Trans-Conductance

The trans-conductance (gm) of devices can be calculated by differentiating the drain-source current with respect to gate-source voltage at a constant drain-source voltage [18]:

gm=∂ID∂VGS|Vds=const                                                        (1)

Gm shows the drain current dependence to gate-source voltage at a fixed drain-source voltage. Figure 5(a) provides a comparison between gm for different NSS and NDS in the proposed and conventional structures at VDS=10V. The displayed gm curve in the structure with NSS=NDS=1×1018cm-3 corresponds to the conventional structure. This figure reveals that maximum gm of the proposed structure with NSS=0.75×1018cm-3 and NDS=1.25×1018cm-3 is larger than those in the other proposed structures while the maximum gm in this structure is equal to that in the conventional structure. As a result from this figure, it is obvious that a larger difference between NSS and NDS causes a significant reduction in the maximum gm. Small difference between NSS and NDS increases the maximum gm. Comparison between maximum gm for different XSS and XDS at VDS=10V is exposed in the figure 5(b). As is discussed in the previous sections, the average of XSS and XDS is similar to that in the conventional (0.32). It is apparent from this figure that the structure with XSS=0.37 and XDS=0.27 and conventional have the maximum gm. The structure with the minimum XSS has the minimum gm. Also, it can be deduced that the structures with smaller XSS than XDS have the lesser maximum gm than the structures with larger XSS than XDS. Therefore, a larger XSS compared to the XDS in the proposed structures can be used to improve the maximum gm.

## Cut Off Frequency

The cut-off frequency (fT) can be calculated from equation (2) where gm is the maximum DC trans-conductance and cgs is the gate-source capacitance [19].

fT=gm2πCgs  (2)                                                                                                                                                           Equation (2) shows that a larger gm/Cgs ratio improves the fT. It can be seen from the figs. 4 and 5 that the structure with NSS=0.75×1018cm-3 and NDS=1.25×1018cm-3 at a fixed XSS and XDS (0.32) has larger gm and smaller Cgs than that in the conventional structure. Therefore, this proposed structure has larger gm/Cgs ratio and consequently larger fT compared to the conventional structure. Also, it is obvious from these figures that the structure with XSS=0.42 and XDS=0.22 has equal gm and smaller Cgs compared to the conventional structure. Hence, this structure improves fT in comparison with that in the conventional structure.

Fig. 4(a)

Fig. 4(b)

Fig. 4. Gate-source capacitances as a function of the frequency for (a) different NSS and NDS at a fixed XSS and XDS (0.32) and (b) different XSS and XDS at a fixed NSS and NDS (1×1018cm-3) in the proposed and conventional structures at VGS=0V and VDS=20V.

Fig. 5(a)

Fig. 5(b)

Fig. 5. Maximum DC Trans-conductance dependence to gate-source voltage for (a) different NSS and NDS at a fixed XSS and XDS (0.32) and (b) different XSS and XDS at a fixed NSS and NDS (1×1018cm-3) in the proposed and conventional structures at VDS=10V.

## Output Conductance

The output conductance (go) of the devices can be calculated by differentiating the drain-source current with respect to drain-source voltage when gate-source voltage is constant.

go=∂ID∂VDS|||VGS=const                                             (3)

It can be concluded from the equation (3) that go shows the drain current dependence to the drain-source voltage for a fixed gate-source voltage. Figure 6(a) shows the output conductance dependence to the NSS and NDS at VGS =-4V in the proposed and conventional structures. In the conventional structure, NSS is equal to the NDS. As is disclosed in this figure, the output conductance of the structures with smaller NSS than NDS is lesser than that in the conventional structure. This is because, as reported in figure 3(a), the drain current versus drain voltage reduces in comparison with the conventional and consequently reduces the output conductance. Also, it can be concluded that in this condition the drain voltage control on the channel is reduced. As is exhibited in this figure, the go in the structures with higher NSS compared to NDS is larger than that in the conventional. So, the drain-source voltage control on the channel is increased in these structures. The minimum go is obtained at the proposed structure with NSS=0.5×1018cm-3 and NDS=1.5×1018cm-3. With increasing drain voltage for different structures, the output conductance is reduced because the drain current is coming near to the saturation region and then slope of the drain current curve is reduced. The go dependence to the drain-source voltage for different XSS and XDS at a fixed NSS and NDS value (1×1018cm-3) is plotted and compared to that in the conventional in the figure 6(b). According to this figure, the proposed structures with smaller XSS than XDS have lesser go than that in the conventional. The smallest go in the investigated structures is obtained for the structure with XSS=0.22 and XDS=0.42. In the structures with bigger XSS than XDS, the go is equal to that in the conventional structure. Therefore, it can be concluded that smaller XSS compared to XDS can be applied to reduce the go.

# Conclusion

Important DC and RF parameters of the AlGaN/GaN HEMTs with step doping concentration or aluminum mole fraction in the barrier are reported in details. The gate-source capacitance, maximum gm, cut off frequency, lateral electric field, breakdown voltage, go and drain current in the proposed structures are studied and compared to those of the conventional structure. Our simulation results disclose that the proposed structures improve the breakdown voltage, gate-source capacitance, cut off frequency and go in comparison with those in the conventional structure. The maximum drain current and gm in the proposed structure is equal to those in the conventional. Also, it is clear that the maximum breakdown voltage of the proposed structures (~220V) is significantly larger than that in the conventional (~90V).

Fig. 6(a)

Fig. 6(b)

Fig. 6. Output conductance as a function of drain-source voltage for (a) different NSS and NDS at a fixed XSS and XDS (0.32) and (b) different XSS and XDS at a fixed NSS and NDS (1×1018cm-3) in the proposed and conventional structures at VGS = -4V.

References

- Y. Ando, Y. Okamoto, H. Miyamoto, T. Nakayama, T. Inoue, and M. Kuzuhara, “10 W/mm AlGaN-GaNHFET with a ﬁeld modulating plate,” IEEE Electron Device Lett., vol. 24, no. 5, pp. 289–291, May 2003.

- Y. F. Wu, M. Moore, A. Saxler, T. Wisleder, and P. Parikh, “40 W/mm double ﬁeld plated GaN HEMTs,” in Proc. Dig. Device Res. Conf., Jun. 2006, pp. 151–152.

- W. Chong, H. Yunlong, Z. Xuefeng, H. Yue, M. Xiaohua, and Z. Jincheng,  “AlGaN/GaNHEMTswith 0.2 µm V-gate recesses for X-band application,” Journal of Semiconductors, Vol. 33, No. 3, pp. 34003-34006, 2012.

- J. Liu, Y. Zhou, J. Zhu, Y. Cai, K.M. Lau, and K. J. Chen, “DC and RF Characteristics of AlGaN/GaN/InGaN/GaN Double-Heterojunction HEMTs,” IEEE Trans. Electron  Devices, Vol. 54, No. 1, pp. 2-10, 2007.

- Y. F. Wu, A. Saxler, M. Moore, R. P. Smith, S. Sheppard, P. M. Chavarkar, T. Wisleder, U. K. Mishra, and P. Parikh, “30-W/mm GaN HEMTs by ﬁeld plate optimization,” IEEE Electron Device Lett., vol. 25, no. 3, pp. 117–119, Mar. 2004.

- Y. Pei, R. M. Chu, N. A. Fichtenbaum, Z. Chen, D. Brown, L. Shen, S. Keller, S. P. DenBaars, and U. K. Mishra, “Recessed slant gate AlGaN/GaN high electron mobility transistors with 20.9 W/mm at 10 GHz,” Jpn. J. Appl. Phys. 2, Lett., vol. 46, no. 45, pp. L1087–L1089, Nov. 2007.

- I. Saidi, Y. Cordier, M. Chmielowska, H. Mejri and H. Maaref, “Thermal Effects in AlGaN/GaN/Si High Elec- tron Mobility Transistors,” Solid-State Electronics, Vol. 61, No. 1, 2011, pp. 1-6.

- M. K. Chattopadhyay and S. Tokekar, “Thermal Model for dc Characteristics of Algan/Gan Hemts Including Self-Heating Effect and Non-Linear Polarization,” Micro- electronics Journal, Vol. 39, No. 10, 2008, pp. 1181-1188.

- R. K. Tyagi, A. Ahlawat, M. Pandey and S. Pandey, “An Analytical Two-Dimensional Model for AlGaN/GaN HEMT with Polarization Effects for High Power Applica- tions,” Microelectronics Journal, Vol. 38, No. 8-9, 2007, pp. 877-883.

- E. J. Miller, “Trap Characterization by Gate-Drain Con- ductance and Capacitance Dispersion Studies of an AlGaN/GaN Heterostructure Field Effect Transistor,” Jour- nal of Applied Physics, Vol. 87, No. 11, 2000, pp. 8070- 8073.

- M. Juncai, Z. Jincheng, X. Junshuai, L. Zhiyu, L. Ziyang, X. Xiaoyong, M. Xiaohua, and H. Yue, “Characteristics of AlGaN/GaN/AlGaN double heterojunction HEMTs with an improved breakdown voltage,” Journal of Semiconductors, Vol. 33, No. 1, pp. 14002-14006, 2012.

- ATLAS user's manual: Device simulation software, Silvaco International,  September 2005.

- S.E.J. Mahabadi, A.A. Orouji, P. Keshavarzi, and H.A. Moghadam, “A new partial SOI-LDMOSFET with a modified buried oxide layer for improving self-heating and breakdown voltage,” Semicond. Sci. Technol., Vol. 26, pp. 95005-950016, 2011.

- A.A. Orouji, S.M. Razavi, S.E. Hosseini, and H.A. Moghadam, “Investigation of the novel attributes in double recessed gate SiC MESFETs at drain side,” Semicond. Sci. Technol., Vol. 26, pp. 115001-115005, 2011.

- C.L. Zhu, Rusli, C.C. Tin, G.H. Zhang, S.F. Yoon, J. Ahn, ”Improved performance of SiC MESFETs using double-recessed structure,” Microelectronic Engineering, Vol. 83, pp. 92–95, 2006.

- J. Zhang , X. Luo, Z. Li, B. Zhang,” Improved double-recessed 4H-SiC MESFETs structure with recessed source/drain drift region,” Microelectronic Engineering, Vol. 84, pp. 2888–2891, 2007.

- S.M. Razavi, S.H. Zahiri, S.E. Hosseini, “A novel AlGaN/GaN HEMT with a p-layer in the barrier,” Physica E, Vol. 54, 2013, pp. 24-29.

- M. K. Verma and B. B. Pal, “Analysis of Buried Gate MESFET Under Dark and Illumination,” IEEE Trans. Electron  Devices, Vol. 48, No. 9, pp. 2138-2142, 2001.

- J. Yang, J. Spann, R. Anderson, and T. Thornton, “High-Frequency Performance of Subthreshold SOI MESFETs,” IEEE Trans. Electron  Devices, Vol. 25, No. 9, pp. 652-654, 2004.