Nanoparticles size detection method based on surface plasmon polaritons in graphene nanopore

Nafiseh Amiri (Student), Bashir Fotouhi (PhD student)

Dept. of Electrical and Computer Engineering Tarbiat Modares University, Tehran, Iran

n.amiri@modares.ac.ir, bashirfutuhi@gmail.com

*Vahid Ahmadi (Professor)

Dept. of Electrical and Computer Engineering Tarbiat Modares University, Tehran, Iran

*v_ahmadi@modares.ac.ir

Abstract— A nanometric plasmonic size detector based on surface plasmon polaritons (SPPs) in graphene is proposed and the excitation of TM surface plasmon polaritons by a point source is simulated by using finite difference frequency domain (FDFD) method. Here we show that in the presence of graphene layer and GaAs as the substrate strong E-filed confinement is achievable. This detector provides the possibility of optical detection of size of the nanoparticles with smaller dimensions than free space wavelength by calculating transmittance of plasmonic wave on the graphene nanopore. There is a nanopore in the middle of structure that the nanoparticle is placed inside it. The SPP wavelength is 17.474nm which is finely matched with 17.101nm theoretical value by simulating in 40 THz frequency. Results show that the transmittance have a relatively linear relationship with nanopore radius and the radius of nanoparticles under detection. Results indicate that the proposed method can detect different nanoparticles with acceptable accuracy to overcome inherent problems in electrical sensing specially for bio sensing applications.

Keywords: Graphene; Surface Plasmon Polariton; Sensor; Nanopore

# Introduction

In recent years graphene has been introduced to the field of plasmonics owing to the fact that it has fundamental properties and potential applications in nanoelectronic and plasmonic such as nano-photonics, biosensing, gap detection, terahertz technology, optics transformation, plasmonic metamaterials, electro-optical modulation, quantum plasmonics, light harvesting and tunable lighting at the nanoscale [1-6]. Graphene is a two-dimensional form of carbon atoms arranged in a honeycomb lattice that turns out to be a gapless semiconductor with fascinating electrical, optical and plasmonic properties [3-8]. Graphene has low loss, flexible feature, good tunability, high quantum efficiency and confinement for light–matter interactions. It is optically nonlinear and contains plasmons with unusual properties [3, 6]. Graphene can support surface plasmon which are quanta of surface charge density oscillations that propagate at the metal–dielectric interface and because the surface charge oscillations are intimately coupled to electromagnetic fields, surface plasmons are polaritons. [9]. The surface plasmons polaritons (SPP) provides strong local field enhancement and confinement, accompanied by an appreciable reduction of the wavelength relative to the  free-space radiation [10]. In this work, the main goal is to reach strongly confined plasmonic wave and use it in nanoparticle detecting devices. The finite difference frequency domain (FDFD) method with using of absorber layers as perfectly matched layers (PML) for the boundary conditions is employed to simulate the propagation of SPPs. Spherical gold nanoparticles with different radiuses are detected by their effect on this highly confined plasmonic wave that transmits through nanopore. Results of this research can be used to discover the possibility of detecting biomolecules by transmission of plasmonic wave.

# Material and Methods

The optical structure which have been designed and simulated is presented in Fig. 1. The structure consists of a graphene of thickness 0.34 nm which is placed on GaAs substrate. Drilling a nanopore in the middle of structure can be done by highly focused electron beam of transmission electron microscopy (TEM) or with heavy ions track lithography method, which allows the energetic ions pass through nanoholes in a mask and then bombard the graphene sheet [11, 12]. The plasmonic wave is excited on graphene by an electric dipole that acts as a point source of SPPs on graphene film and transmits through a nanopore to the second part of the structure. The intensity of plasmonic-wave power and s-parameters are calculated to detect size of the sensing material. Here we try to calculate the sensitivity through involving S-parameters which include information regarding the reflected and incident power waves between the ports of the device. For a two port device there are four S-Parameters S11,  S12, S21 andS22. The S11 and S22 are simply defined as the forward and reverse reflection coefficients of electromagnetic wave and also  S12 and S21 are simply defined as the forward and reverse transmittances coefficients of electromagnetic wave. We have chosen this method because a change Δr in the radius of the nanoparticle, influences the transmitted power and S-parameters. Radius modulation can be detected by either tracking the transmittance or monitoring the S-parameters at a fixed frequency. The use of this principle allows designing ultra-small plasmonic sensors that can detect analytes (e.g. bio molecules). The sensitivity of the detector can be defined as the slope of power or S-parameters:

| SP=∂P∂r | (1) |
| --- | --- |

| SS21=∂S21∂r | (2) |
| --- | --- |

where P is the transmitted power of cross section, S21 is transmittance coefficient and r is the nanoparticle radius.

Figure 1. Schematic of monolayer graphene on GaAs substrate. Nanoparticle is depicted as yellow sphere. a) three dimensional cut plane. b) y-z cut plane.

# Results

We analyze the interaction of an electromagnetic source and graphene by using FDFD method. The electromagnetic fields are governed by Maxwell’s equations and graphene is represented by a conductivity surface [1]. Graphene is modelled as an infinitesimally-thin, local two-sided surface characterized by a surface conductivity σ (ω, µ, Г,T) where ω is angular frequency, µ is chemical potential, Г is a phenomenological scattering rate and T is temperature. We use Kubo formula to define graphene conductivity  [1]:

| ω,u, Γ,T=je2ω-j2Γπℏ2× 1ω-j2Γ2 0∞ϵ∂fd(ϵ)∂ϵ-∂fd(-ϵ)∂ϵdϵ-0∞fd(-ϵ)-fd(ϵ)ω-j2Γ2-4ϵℏ2 dϵ |  |
| --- | --- |

where e is the charge of an electron, ℏ=h/2π is the reduced Planck’s constant, kB is the Boltzmann’s constant, ω is radian frequency, Γ is phenomenological scattering rate, u is chemical potential, ϵ is energy  and fdϵ=1/eϵ-ukBT+1 is the Fermi-Dirac distribution.

Next we investigate the propagation of SPP waves onto the graphene by considering water (n=1.33) as background and assuming that chemical potential remains constant at µ=0.2 eV. We use absorbing layers to prevent the reflection of the plasmonic wave from the end of the graphene. The simulation is done in frequency domain at 40 THz.

Logarithmic profile of the one dimensional of the z component of the electric field for the simple structure (without nanopore and nanoparticle), with nanopore structure (without nanoparticle) and with  nanoparticle structure are represented in Fig. 2. The inset   shows the three-dimensional profile of the E-field along propagation direction for the nanoparticle structure; where plasmon is strongly confined. The SPP wavelength is 17.474 nm that finely matches with 17.101 nm theoretical value.

Fig.3 shows the distribution of the z component along y direction for electric field for the simple structure (without nanopore and nanoparticle), nanopore structure (without nanoparticle) and nanoparticle structure. As we expected E-field is decreasing exponentially away from the interface into the directions ±y. As demonstrated in Fig.3 that best vertical confinement occurs for the simple structure and drilling nanopore and putting nanoparticle makes it so weaker.

The S21 is defined as,

| S21=power deliverd to output port ( port 2)power incident on input port ( port 1) | (4) |
| --- | --- |

We consider electrical dipole as input discrete port and put a rectangular wave guide port at the distance of 50nm from the nanopore as output port. The magnitude of S21  gives the transmittance. To obtain S21 we have to calculate power. Power is calculated by,

| P=12 ϵ0Vp -∞∞E2dxdy | (5) |
| --- | --- |

where Vp  is the phase velocity of plasmonic wave [13]. For simplicity, we limit the power calculation to x= [-30nm, 30nm] and y= [-15nm, 15nm]. Simulation results show that in simple structure transmittance is relatively high but in nanopore structure, as the nanopore radius increases, the transmittance decreases due to disturbing effect of nanopore on SPP characteristics. Also we can see decreasing rate is slower at bigger radiuses and in smaller radiuses, sensitivity is much better. But it should be noted that in very small radiuses, drilling procedure and transmitting biomolecules through such small pores gets more difficult. So we consider the radius to be 12 nm and 10 nm as optimized pore radius for sensing, because in these radiuses sensitivity is reached to an acceptable value.

Next we insert a gold spherical nanoparticle into the pore and repeat simulations for different nanoparticle radiuses. Fig.4 represents the relationship between the transmitted power and nanoparticle radius. We calculate power by use of Eq. (5).

Figure 2. Logarithmic profile of the z component of the electric field distribution at 40 THz for simple structure (dashed line), with nanopore structure (solid line) and with nanoparticle structure (dashed-dotted line). The inset is three dimensional profile of the E-field distribution for nanoparticle structure.

Fig. 5 shows the relationship between S21 and nanoparticle radius for both of pore radiuses and Fig. 5 shows the relationship between transmitted power and nanoparticle radius for both of pore radiuses. It is seen from these results that increasing the nanoparticle radius increases S21 due to filling the pore with nanoparticle and decreasing the disturbance of the pore. When nanoparticle radius is almost equal to the nanopore radius we see increase in power and transmittance coefficient or S21.We calculate sensitivities SS21=0.586×10-6  nm-1 and SS21=0.469×10-6  nm-1 from Eq. (2) for 12nm pore radius and 10nm pore radius respectively.

Figure 3. One-dimensional profile of the z component of the electric field distribution along y direction at 40 THz for simple structure (dashed- dotted line), nanopore structure (dashed line) and nanoparticle structure (solid line).

Figure 4. Effect of particle radius on s-parameter for the pore radius of 10nm (solid line) and pore radius of 12nm (dashed line).

Figure 5. Effect of particle radius on power for the pore radius of 10nm (solid line) and pore radius of 12nm (dashed line).

IV.      CONCULUSION

In summary, we presented an analysis on the graphene nanopore structure to detect a small change in the radius of a nanoparticle at the center of the graphene nanopore. We have shown that SPP waves on graphene can be strongly confined in nanometer scales. We found that 12 nm and 10 nm are the optimized radius for our nanopore structure. The sensitivity was obtained 586 m-1 for 12 nm pore radius and 467 m-1 for 10 nm pore radius.

##### References

[1] G. W. Hanson, "Dyadic Green’s functions and guided surface waves for a surface conductivity model of graphene," Journal of Applied Physics, vol. 103, p. 064302, 2008.

[2] H. Lu, C. Zeng, Q. Zhang, X. Liu, M. M. Hossain, P. Reineck and M. Gu, "Graphene-based active slow surface plasmon polaritons," Scientific Reports, vol. 5, 2015.

[3] A. Grigorenko, M. Polini, and K. Novoselov, "Graphene   plasmonics," Nature Photonics, vol. 6, pp. 749-758, 2012.

[4] S. D. Sarma, S. Adam, E. Hwang, and E. Rossi, "Electronic transport in two-dimensional graphene," Reviews of Modern Physics, vol. 83, p. 407, 2011.

[5] K. F. Mak, L. Ju, F. Wang, and T. F. Heinz, "Optical spectroscopy of graphene: from the far infrared to the ultraviolet," Solid State Communications, vol. 152, pp. 1341-1349, 2012.

[6] X. Luo, T. Qiu, W. Lu, and Z. Ni, "Plasmons in graphene: Recent progress and applications," Materials Science and Engineering: R: Reports, vol. 74, pp. 351-376, 2013.

[7] M. Katsnelson and K. Novoselov, "Graphene: New bridge between condensed matter physics and quantum electrodynamics," Solid State Communications, vol. 143, pp. 3-13, 2007.

[8] A. K. Geim and K. S. Novoselov, "The rise of graphene," Nature Materials, vol. 6, pp. 183-191, 2007.

[9] A. Bouhelier and L. Novotny, "Near-field optical excitation and detection of surface plasmons," in Surface Plasmon Nanophotonics, ed: Springer, 2007, pp. 139-153.

[10] P. Alonso-González, A. Nikitin, F. Golmar, A. Centeno, A. Pesquera, S. Vélez, et al., "Controlling graphene plasmons with resonant metal antennas and spatial conductivity patterns," Science, vol. 344, pp. 1369-1373, 2014.

[11] W. Li, L. Liang, S. Zhao, S. Zhang, and J. Xue, "Fabrication of nanopores in a graphene sheet with heavy ions: A molecular dynamics study," Journal of Applied Physics, vol. 114, p. 234304, 2013.

[12] G. F. Schneider, S. W. Kowalczyk, V. E. Calado, G. Pandraud, H. W. Zandbergen, L. M. Vandersypen and C. Dekker, "DNA translocation through graphene nanopores," Nano Letters, vol. 10, pp. 3163-3167, 2010.

[13] D. K. Cheng, Field and wave electromagnetics vol. 2:   Addison-Wesley New York, 1989.