Curvature effects on the electronic and optical properties of single-walled silicon nanotube within tight-binding model

M. Heidari

PhD student

Dept. of Electrical Engineering

Tarbiat Modares University

Tehran, Iran

mh.heidari@modares.ac.ir

V. Ahmadi

Professor

Dept. of Electrical Engineering

Tarbiat Modares University

Tehran, Iran

*v_ahmadi@modares.ac.ir

S. Darbari

Assistant-professor

Dept. of Electrical Engineering

Tarbiat Modares University

Tehran, Iran

s.darbari@modares.ac.ir

Abstract—In this paper, we investigate the curvature effects on the electronic band structure and dielectric function of single-walled silicon nanotubes based on tight-binding method. The curvature nature of nanotubes causes radius-dependent σ-π-orbital hybridization which leads to optimization of tight-binding  model for each radii. First, the effects of orbitals overlap and the structural optimization on the electronic band structure of small radius nanotubes are investigated. Second, the imaginary part of dielectric function of nanotubes, which is related to optical absorption coefficient, is obtained by calculating the interband optical matrix elements using gradient  approximation. It is shown that the σ-π-tight-binding model optimization due to the curvature effects, introduces small changes to the optical transition energies obtained by simple π-band tight-binding model. The results show that the curvature effects are more important in small radius tubes.

Keywords-silicon nanotube; silicene; curvature effect; electronic properties; optical properties

# Introduction

Carbon nanotubes (CNTs) were synthesized in 1991 and in last decade, significant effort have been attracted to their amazing properties. After carbon nanotubes, other types of nanotubes such as BN, GaN and AlN have been studied theoretically and experimentally synthesized [1]. Two dimensional Silicon (Si) hexagonal honeycomb lattice was proposed as silicene, recently. Silicene also has a lattice like graphene sheet, which exhibit a linear dispersion. Si atoms of silicene in  honeycomb lattice have sp2 configuration. When a two dimensional sheet of  silicon is rolled up along a chiral vector, Si nanotubes is created.

In this work, we apply Tight-binding (TB) model to study Silicon nanotube's (SiNT) band structure which have been done previously by accurate ab-initio calculation [2]. Also TB model was applied to the similar two dimensional materials like CNTs and graphene, successfully. In silicene sheet, sp2 hybrid orbitals lie on the same plane, make three σ-bonding, and the remaining out-of-palne pz-orbitals of silicon atoms, make π-bonding. In case of  SiNT, atomic orbital rearranges in sp3 hybridization and simple π-TB model, based on single orbital per atom, is no longer valid [3]. So more complicated model should be used. Our TB model is based on a mixture of  four atomic orbitals: 3s, 3px, 3py and 3pz.

The curvature of SiNT's wall, modifies the angle of  hybrid sp3 orbitals bonds and depends on SiNT's radius [4-5]. Radius-dependent σ-π-orbital hybridization changes the atomic orbitals overlap [6]. The deviation from the sp2 hybridization alter electronic properties of SiNTs and the curvature effect is more significant in the case of narrow nanotubes compared to the simple π-TB model.

After calculation of electronic band structure of SiNTs, their optical properties have been treated within π-TB and σ-π-TB models [7]. The optical transition can be obtained from optical matrix elements of the linear momentum for interband transitions. The dielectric function of SiNTs is calculated using gradient approximation [8].

Our paper is organized as follows: in Sec. II we describe σ-π Tight-binding model for two dimensional materials like CNT and SiNT, then we employ TB model to obtain optical transition rules and optical properties of SiNTs. In Sec. III, we present results and discussion, and finally in Sec. IV we provide concluding remarks.

# Methods

## Nantube structure

The SiNT can viewed as silicene sheet rolled up around a certain vector, which determine nanotube's diameter. The structure of silicene consist of two sub-lattice, A and B, as seen in Fig. 1. In silicene three orbitals, 3s, 3px and 3py hybridize in an sp2 configuration and forming σ bonds, whereas the other 3pz  orbitals only participate in π bond. The lattice constant length of silicene, a0 is about 3.82 Å [1,2]. Notice that the basis vector and Brillouin zone of silicene are similar to that of graphene.

## Tight-binding model

The TB model has moderate precision and can be combined with the other method to enhance the accuracy. TB model is based on an approximate set of wave functions which are a superposition of isolated atomic orbitals and describes the properties of tightly bound electron in solids.

As a sheet of silicene is rolled up to construct a SiNT, orbitals are hybridized into sp3 configuration and all orbitals participate in π and σ bonding. So it is necessary to take account all orbitals in our TB model [6]. we consider four orbitals per atom and the Hamiltonian matrix size is four times of Si atoms in the unit cell. The wave functions sub-lattice A/B can be expressed as linear combinations of atomic wave functions as:

| ψA/B , α, k=1N i=1Neik.Ri ¦Ri, A/B, α⟩ | (1) |
| --- | --- |

Fig. 1. Lattice of a silicene sheet

where 𝛼 = s, px, py, pz are atomic orbitals, Ri is a lattice vector of honeycomb lattice, k is wavenumber and N is the number of the atomic wave function in the unit cell.

In our TB model we use the first nearest neighbor TB parameters, were taken from previous ab-initio calculations [1]. The TB parameters are given in Table 1.

- Table 1. Tight-binding parameters for Si sheet . [1]

| parameter | Hopping integral |
| --- | --- |
| (ssσ)1AB | -2.066 |
| (spσ)1AB | 2.1184 |
| (ppσ)1AB | 3.1866 |
| (ppπ)1AB | -0.8867 |

## Optical properties

Most of the works on the optical properties of CNTs is based on π-TB model. The selection rules for allowed dipole interband transition discussed by Ajiki [7]. In the same manner, we calculate dielectric function of SiNTs within π-TB model. Then we consider the effect of σ-π-hybridization in our TB model and inclusion of the curvature effect. By assuming that the wave vector of the optical field is negligible compared to the electronic wave vector, the dipole operator ψcE.pme ψv   is evaluated within gradient approximation to ψc∂H∂k ψv  , where ψc and ψv are conduction and valance wave functions, p is linear momentum operator and me is electron mass [8].

# Result and Discussion

    - The TB model is used for electronic band structure and dielectric function calculation of some small-radius  SiNT. The effect of curvature on band structure and optical transition energies have been investigated based on σ-π-TB calculation. As shown in Fig. 2, the calculated electronic band structure for SiNT (4,0) within π-TB model without curvature effect, exhibits major differences from that of π-TB and σ-π-TB model with inclusion of the curvature effect. Fig. 2(a) shows the π-bands of SiNT (4,0) in sp2 configuration. Fig.2 (b) shows only the π-bands of SiNT (4,0) in sp2 configuration and the curvature effect have been considered. Obviously curvature effect alters the band structure of simple sp2 configuration. Curvature induced σ-band and π-band mixing is presented in Fig. 2(c).

Curvature-induced rehybridization has larger effects in thinner SiNTs and decreases for thicker tubes. As shown in Fig. 3(a), SiNT (3,0) seems to be metallic (zero-gap semiconductor) in π-TB model,  but the curvature effect, opens the gap. The effect of curvature on the energy gap, plotted versus SiNT radius in Fig. 3(b) and compared with simple π-TB model.

Fig. 4.  Comparison of Energy gap with and without curvature effect. (a) SiNT (3,0). (b) as a function of tube radius.

(4,0) π-TB

Use

Fig. 3. Band structure of SiNT (4,0) obtained from our TB model.

In the presence of electromagnetic illumination on nanotube, the electrons are excited from occupied valance bands into the empty conduction bands. The optical absorption spectra is derived from the imaginary part of dielectric function and plotted for some different radius. The dielectric function calculated within π-TB model and σ-π-TB model, and the effect of curvature on the dielectric function are investigated. The results are shown in Fig. 4. As seen in Fig. 4 (a), the dielectric function of SiNT (4,0) shows two peaks, the lowest peak located below 1eV energy and the other peak at about 1.8 eV.  The results show that the curvature strongly affects the lower  peak. In the case of SiNT (4,0), inclusion of the curvature effect, causes a red shift in absorption spectra, but in general case, there is no rule.

Fig. 4 (b) shows the dielectric function of three SiNTs, (3,0), (4,0) and (5,0) within σ-π-TB model and inclusion of the  curvature effect. In the case of SiNT (3,0), which thought to zero gap semiconductor,  curvature effect opens the gap and blue shift occurs in the dielectric function. The presence of two close peaks in the curves can be explained with the curvature-induced σ-π-rehybridization.

Fig. 4. The dielectric function of SiTNs within TB model. (a) dielectric function of SiNT (4,0) in π-TB, σ-π-TB model with and without curvature effect. (b) the dielectric function of (3,0), (4,0) and (5,0).

(a)

(4,0) π-TB with Curvature effect

(b)

(4,0) σ-π-TB with Curvature effect

(c)

(a)

x

Γ

(3,0)

(b)

(a)

(4,0)

x

Γ

(5,0)

(b)

# Conclusion

In this paper, the effect of structural curvature on the electronic band structure and optical properties of small radius SiNTs, band structure and energy gap of SiNTs are studied within π-TB model and σ-π hybridized TB model. It is shown that the calculated electronic band structure and the dielectric function of small radius SiNTs exhibit large differences with the simple π-TB model. The derived dielectric function of small SiNTs differ from sp2 configuration π-TB model due to the curvature effect. The difference optimized and nonoptimized TB model, decrease with the increase of SiNT radius and can be ignored for large nanotube radius.

##### References

[1]  G. G. Guzmán-Verri and L. L. Y. Voon, “Electronic structure of silicon-based nanostructures,” Phys. Rev. B, vol. 76, no. 7, p. 075131, 2007.

[2]  A. Kara, H. Enriquez, A. P. Seitsonen, L. L. Y. Voon, S. Vizzini, B. Aufray, and H. Oughaddou, “A review on silicene—new candidate for electronics,” Surf. Sci. Rep., vol. 67, no. 1, pp. 1–18, 2012.

[3]  J. D. Correa, A. J. da Silva, and M. Pacheco, “Tight-binding model for carbon nanotubes from ab initio calculations,” J. Phys. Condens. Matter, vol. 22, no. 27, p. 275503, 2010.

[4]  V. Bezugly, H. Eckert, J. Kunstmann, F. Kemmerich, H. Meskine, and G. Cuniberti, “Quantification of curvature effects in boron and carbon nanotubes: Band structures and ballistic current,” Phys. Rev. B, vol. 87, no. 24, p. 245409, 2013.

[5]  V. N. Popov, “Curvature effects on the structural, electronic and optical properties of isolated single-walled carbon nanotubes within a symmetry-adapted non-orthogonal tight-binding model,” New J. Phys., vol. 6, no. 1, p. 17, 2004.

[6]  B. Gharekhanlou and S. Khorasani, “An overview of tight-binding method for two-dimensional carbon structures,” Graphene Prop. Synth. Appl., pp. 1–37, 2011.

[7]  V. N. Popov and L. Henrard, “Comparative study of the optical properties of single-walled carbon nanotubes within orthogonal and nonorthogonal tight-binding models,” Phys. Rev. B, vol. 70, no. 11, p. 115407, 2004.

[8]  R. Alaei and M. H. Sheikhi, “Optical Absorption of Graphene Nanoribbon in Transverse and Modulated Longitudinal Electric Field,” Fuller. Nanotub. Carbon Nanostructures, vol. 21, no. 3, pp. 183–197, 2013.